GTY-1002

GM-1002 is composed of Aramid fiber,non asbestos mineral fiber,synthetic fiber,with nitrle butadiene rubber binder(NBR) by Beater.It exhibits excellent crush resistance at high-flange pressures.Recommended for sealing oil,fuels and water in applications with intermittent operating temperatures up to 200℃.Applications include general automotive,motorcycle,small engine and Motor sealing .

Properties

| NO. | item | unit | standard values |
| --- | --- | --- | --- |
| 1 | Transverse tensile strength | MPa | ≥10 |
| 2 | Compressibility | % | 15-30 |
| 3 | Recovery | % | ≥40 |
| 4 | Density | g/cm3 | ≥1.20 |
| 5 | Flexiblity （Bend 180° on the bar with diameter which is 12 times than the sample thickness ） | No crack |
| 6 | Creep Relaxation | % | ≤35 |
| 8 | Immersed into IRM903 oil for 5h at 150℃±2℃，then pick up and keep it for 30min at 15℃-30℃ | Transverse tensile strength | MPa | ≥8 |
| 9 |  | Thickness increase | % | ≤20 |
| 10 |  | Weight increase | % | ≤35 |
| 11 | Immersed into ASTM B for 5h at 21℃~30℃ | Thickness increase | % | ≤20 |
| 13 |  | Weight increase | % | ≤40 |
| 14 | Immersed into H2O for 5h at 100℃±2℃ | Weight increase | % | ≤40 |
| 16 |  | Thickness increase | % | ≤20 |
| 17 | Nitrogen Sealing ［ml/（h·mm）］ | ≤500 |
| 18 | Sealability for oil at room Temperature （Medium pressur 8mpa,30min） | No leakage within 30 minutes |